
**Reviewer’s Comments**

****

**Long Chain Polymeric Carbohydrate dependent nanocomposites in tissue engineering**

**Abstract**

**Introduction**

The use of nano-medicine has increased enormously especially in the field of gene delivery and targeted drug delivery. Ithas gained a lot of interest due to its wide application. Physical and chemical attributes of nanomaterials have lengthened its application in the field of biological science, and biomedical engineering such as biological imaging, drug delivery, bio-molecular sensing, and Infectious Diseases(X. Wang, Liu, Ramstrom, and Yan, 2009). There are different types of nanomaterials such as Inorganic nanomaterials (Graphene, mesoporous silica, gold, magnetic, quantum dots, and layered double hydroxides) and metal-organic frameworks (Zirconium-based metal-organic frameworks,Lanthanide-Based Metal-OrganicFrameworks,Oligonucleotide-Functionalized Metal-Organic Framework) (S. Wang *et al*., 2017)(Pagis, Ferbinteanu, Rothenberg, and Tanase, 2016)(Liang, Wei, Evans, and Duan, 2014)(Schaate *et al*., 2011). Inorganic nanomaterials possess intrinsically physicochemical properties and good biocompatibility, as a result, they are used in different applications such as bio imaging, targeted drug delivery and cancer therapies whereas Metal-organic framework is porous hybrid polymer-metal composites. They possess many biomedical applications due to its excellent porosity, high loading capacity, biodegradability and ease of surface modification when compared to among others (Beg *et al*., 2016)(Keskin and Kızılel, 2011).

The selection of material depends upon biologically activity, biocompatibility and biodegradability. The materials provide analogous environment to the extra cellular matrix (ECM) and provide an induced rate of synthesis or growth of new tissues.Extracellular matrix consists of collagen fibril, glycoproteins such as fibronectin and laminin for attachment. In addition to the extracellular matrix, connective tissues are characterized by fibroblasts, and ground substance which are usually fluid in nature but it can also be mineralized and solid, as in bones(Kusindarta and Wihadmadyatami, 2018).

Polysaccharides offer a green alternative to synthetic polymers in the preparation of soft nanomaterials (Zheng, Monty, and Linhardt, 2015).These are Polymeric carbohydrate molecules consisting of long chains of monosaccharide or disaccharide units are linked together covalently by glycosidic linkages. In addition to monosaccharides, they may also contain other components such as methyl, sulfate and pyruvate. They may have a branched or linear molecular structure. The bacterial polysaccharides can be subdivided into the exopolysaccharides, capsular polysaccharides and the intracellular polysaccharide. Xanthan, dextran, alginate, gellan and hyaluronicacid (HA) are examples of exopolysaccharides which are synthesized extracellularly by cell wall-anchored enzymes(Mokhtarzadeh, Alibakhshi, Hejazi, Omidi, and Ezzati Nazhad Dolatabadi, 2016)(Mokhtarzadeh, Alibakhshi, Yaghoobi, *et al*., 2016)(Rehm, 2010).

Ismail *et al*., 2018 prepared gellan gum incorporated TiO2 nanotubes using solvent casting method for skin tissue engineering. TiO2 nanotubes are a promising tool for cell growth and proliferation for wound healing (Ismail, Mat Amin, and Razali, 2018). They are biocompatible inosseointegration(Awad, Edwards, and Morsi, 2017) and attenuate inflammatory mediators (Cimpean, Neacsu, Mazare, and Schmuki, 2015). Aadil*et al*., 2019 formulate poly(vinyl) alcohol-gellan gum based nanofiber using electrospinning and found a promising 3D nanofibrous scaffolds for various tissue engineering applications (Aadil, Nathani, Sharma, Lenka, and Gupta, 2019). poly (d, l-lactide-co-glycolide acid) (PLGA) nanofiber is alternative biodegradable polymer when compared with polysaccharide based nanofiber, which used in medical devices and drug delivery applications (Stachewicz *et al*., 2015). Gellan and PVA crosslink nanofiber is prepared to enhance the physiochemical stability and made biocompatible to human dermal fibroblast (3T3L1) cells (Vashisth and Pruthi, 2016).

Cellulose nanocrystals offers aggrandize Cytocompatibility and improved mechanical properties as compared to carbon or metallic nanotubes (Habibi, Lucia, and Rojas, 2010). Nanocellulose reinforced gellan-gum hydrogels is helpful in Annulus fibrosus (AF) defects such as annular tears, herniation and discectomy (Pereira *et al*., 2018).Nanocellulose Composite for also useful in the tumor-targeted gene delivery. Anirudhan and Rejeena have developed a novel nonviral gene vector consist of aminated b-cyclodextrin modified carboxylated magnetic cobalt/nanocellulose composite, which is helpful in reducing the toxicity but also increased the transgene expression level (Anirudhan and Rejeena, 2014). Yvette and co-researcher also worked on nanocellulose based gene delivery and designed polyelectrolyte layer assembly of bacterial nanocellulose whiskers with plasmid DNA (Pötzinger *et al*., 2018). Nguyen *et al*., developed nanocellulose/alginate Bioink for 3D Bioprinting of iPS Cells. The result suggests to support cartilage production in co-cultures with irradiated chondrocytes (Nguyen *et al*., 2017). The other researcher also supports the evidence for the development of 3D bio printing using nanocellulose such as 3D bioprinting of human chondrocyte-laden nanocellulose hydrogels for patient-specific auricular cartilage regeneration (Martínez Ávila, Schwarz, Rotter, and Gatenholm, 2016), wood-based nanocellulose and bioactive glass modified gelatin–alginate bioinks for 3D bioprinting of bone cells (Ojansivu *et al*., 2019) and development of nanocellulose-based bioinks for 3D bioprinting of Soft Tissue. The problem in all above research is lacking pre-clinical and clinical trials. This leads to motivation for researchers to design randomized double blind clinical trial for future commercial prospective.

Dextran based hydrogel is a popular in different kind of tissue repair such as cartilage tissue engineering (Xiaoyu Wang *et al*., 2017), vascular tissue engineering (Y. Liu and Chan-Park, 2009), bone tissue engineering(Ding *et al*., 2019), skin tissue engineering , (Pan, Liu, Sun, and Xu, 2014), wound repair (Ribeiro, Morgado, Miguel, Coutinho, and Correia, 2013). Nikpour and their co researcher developed dextran based bioactive glass-ceramic nanocomposite scaffold. They synthesized nano bioactive glass ceramic particles (nBGC) by sol–gel method whereas chemical cross linked technique is used for the preparation of nanocomposite scaffold. They identify silicon dioxide improves surface reaction to contact with body fluids and develops active surface area for *in vitro/v*ivo bone tissue engineering (Nikpour *et al*., 2018). Some important Polysaccharide-based Nanocomposites for tissue engineering and gene delivery are mentioned in table 1. The researcher excluded a number of nanocomposite as of lack of available literature on *in-vitro* or *in-vivo* evaluation.

Chitosan based biomaterial has been well known for the preparation of nontoxic, biodegradable, and biocompatible polysaccharide of β(1-4)-linked d-glucosamine and N-acetyl-d-glucosamine (Riva *et al*., 2011). Chitosan have been used to prepare collagen/chitosan porous scaffolds (Ma, 2003), injectable chitosan-based hydrogels (R. Jin *et al*., 2009), chitosan-nanohydroxyapatite composite scaffolds (Thein-Han and Misra, 2009), chitin-based tubes (Freier, Montenegro, Shan Koh, and Shoichet, 2005), chitosan-alginate hybrid scaffolds (Z. Li, Ramay, Hauch, Xiao, and Zhang, 2005) and chitosan/carbon scaffolds (Martins *et al*., 2014).

Table 1: Long Chain Polymeric Carbohydrate dependent nanocomposites in tissue engineering

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **No.** | **Material Composition** | **Characterization Techniques** | **Application** | ***In-vitro/in-vivo* Testing relevant to TE and GD** | **Reference** |
| 1. | Gellan gum incorporated TiO2 nanotubes | FTIR, XRD  and SEM | Skin tissue  engineering | Cell viability and proliferation testing | (Ismail *et al*., 2018) |
| 2. | Poly(vinyl) alcohol-gellan gum based nanofiber | SEM and FTIR | 3D nanofibrous scaffold. | *In-vitro* embryonic stem cells (ESCs) | (Aadil *et al*., 2019) |
| 3. | Crosslinked gellan/PVA nanofibers | FESEM | Human dermal fibroblast (3T3L1) cells in tissue engineering application | Cell proliferation behaviour of human dermal fibroblast cells (3T3L1) | (Vashisth and Pruthi, 2016) |
| 4. | Nanocellulose reinforced gellan-gum hydrogels | TEM | Annulus fibrosus tissue regeneration | Bovine annulus fibrosus culture | (Pereira *et al*., 2018) |
| 5. | Dextran and sol–gel derived bioactive glass ceramic nanoparticles | FESEM, SEM | Bone tissue engineering | Normal human osteoblasts (HOB) Cells,  Cell viability assay | (Nikpour *et al*., 2018) |
| 6. | Aminated β-Cyclodextrin-Modified-Carboxylated Magnetic Cobalt/Nanocellulose Composite | FTIR,XRD,SEM,ESR | Tumor Targeted Gene delivery | DNA Binding Studies, MTT Cytotoxicity Assay, *In vitro*Gene Transfection and Gene Expression Experiments. | (Anirudhan and Rejeena, 2014) |
| 7. | 3D Bioprinting of iPS Cells in a Nanocellulose/Alginate Bioink | Confocal images, Fluorescence microscopy | BioprintingiPSCs to support cartilage production in co-cultures with irradiated chondrocytes | Immunohistochemical analysis, Microscopy,Gene expression assays | (Nguyen *et al*., 2017) |
| 8. | Chitosan-chitin nanocrystal composite scaffolds | SEM, XRD | Bone tissue engineering | Cell adhesion and proliferation | (M. Liu *et al*., 2016) |
| 9. | Sodium alginate-xanthan gum based nanocomposite scaffolds | FESEM | Bone tissue engineering | Cell viability | (Kumar, Rao, and Han, 2017) |
| 10. | Nano-hydroxyapatite Pullulan/dextran polysaccharide composite | ESEM | Orthopaedic and maxillofacial surgical applications. | Experimental models performed in rat and goat | (Fricain *et al*., 2013) |
| 11. | Chitosan/Carbon nanofibers Scaffolds | SEM | Cardiac Tissue Engineering | Culture of Neonatal Rat Cardiomyocytes, Gene Expression | (Martins *et al*., 2014) |
| 12. | Nano-bio composite scaffold of  chitosan–gelatin–alginate–hydroxyapatite | ESEM | Bone tissue-engineering | *In vitro* cell culture using osteoblast cell line,Cell viability, proliferation and attachment over the scaffold,Gene expression study, RNA extraction study | (Sharma, Dinda, Potdar, Chou, and Mishra, 2016) |
| 13. | Alginate/gelatin scaffolds with homogeneous  nano apatite coating | SEM, EDS | Bone tissue engineering. | Proliferation and differentiation of cells on scaffolds The | (Luo, Li, Qin, and Wa, 2018) |
| 14. | Nano-hydroxyapatite-alginate-gelatin microcapsule as |  | Modular bone tissue engineering | Osteogenesis activity | (Nabavinia, Khoshfetrat, and Naderi-Meshkin, 2019) |
| 15. | Poly(ε-caprolactone)/keratin nanofibrous mats | SEM | Vascular tissue engineering | Fibroblast viability assay, Cell attachment | (Y. Li, Wang, Ye, Yuan, and Xiao, 2016) |
| 16. | Keratin nanoparticles-coating electrospun PVA nanofiber | SEM | Neural tissue applications | Cell morphology, adhesion and proliferation | (Guo *et al*., 2019) |
| 17 | Nano-hydroxyapatite/chitosan/chondroitin sulfate/hyaluronic acid | SEM | Bone tissue engineering | Cell biocompatibility | (Hu *et al*., 2017) |
| 18 | Chitosan/chondroitin sulfate/nano-bioglass | XRD, FT-IR, FE-SEM and TEM. | Bone tissue engineering | *In-vivo* bone regeneration study, *In-vitro* cell study | (Singh *et al*., 2019) |

**2. Medicinal herbs incorporated into long chain polymeric carbohydratebased Nano-composites**

Plants are the essential foundation of medicine. Some important drugs that are still in use today are derived from traditional medicinal herbs (Aslam and Ahmad, 2016). Functional polysaccharides have a wide variety of application in the field of biomedical engineering and tissue repair (Q. Li, Niu, Xing, and Wang, 2018). A number of medicinal herbs such as *Indigoferaaspalathoides*, *Azadirachtaindica,Memecylonedule* and *Myristicaandamanica* along with a biodegradable polymer, polycaprolactone has been used in combination for skin tissue engineering (G. Jin *et al*., 2013). Table 2 represent some of the medicinal herbs that is used in combination with polysaccharides based Nano-composites. *Lycium barbarum* polysaccharides has encapsulated Poly lactic-co-glycolic acid Nanofibers is indicated for peripheral nerve tissue engineering (J. Wang *et al*., 2018).*Elaeagnus angustifolia* is traditionally indicated in osteoarthritis (Mahboubi, 2018).*Elaeagnus angustifolia* extract was loaded in poly(ɛ-caprolactone)-poly(ethylene glycol)-poly(ɛ-caprolactone) (PCL-PEG-PCL/EA) nanofibers for bone tissue engineering (Hokmabad *et al*., 2019). Aloe vera is incorporated in poly(ε-caprolactone)/gum tragacanth nanofibers to develop the wound dressing (Ranjbar-Mohammadi, 2018).*Stryphnodendron adstringens* is indigenous to Brazil and a well-known wound healing herb in the eastern coast of South America (Hernandes, Pereira, Palazzo, and Mello, 2010). It has been used in combination with Polyvinyl alcohol and pineapple nanofibers for medical applications (Costa *et al*., 2013) .

**Table 2: Some medicinal herbs incorporated into long chain polymeric carbohydratebased Nano-composites for Tissue Regeneration**

|  |  |  |  |
| --- | --- | --- | --- |
| **Medicinal Herb** | **Polysaccharides based Nano-composites** | **Application** | **Reference** |
| *Lycium barbarum* | *Lycium barbarum* polysaccharide encapsulated Poly lactic-co-glycolic acid Nanofibers | Peripheral nerve  tissue engineering | (J. Wang *et al*., 2018) |
| *Elaeagnus angustifolia* | EA extract was loaded onto poly(ɛ-caprolactone)-poly(ethylene glycol)-poly(ɛ-caprolactone) (PCL-PEG-PCL/EA) nanofibers | Bone tissue engineering | (Hokmabad *et al*., 2019) |
| *Aloe barbadensis miller* | Aloe vera incorporated poly(ε-caprolactone)/gum tragacanth nanofibers | Wound dressing | (Ranjbar-Mohammadi, 2018) |
| *Stryphnodendron adstringens* | PVA/pineapple  nanofibers/*Stryphnodendron adstringens* | Medical Application | (Costa *et al*., 2013) |

**3. Clinical trials of long chain polymeric carbohydratebased Nano-material**

Limited available literature on clinical trial of polysaccharides based Nano-material. Although a number of material is available and examined *in-vitro* or *in-vivo* but a very few materials went for clinical trial. Most of available literature does not able to proceed further for clinical trials. A Pilot randomized clinical trial of a customized nanotextile wet garment treatment were performed on moderate and severe atopic dermatitis and found good in the treatment of eczema (He, Koh, Lee, and Ang, 2020). A couple of randomized double blind clinical trial have been performed on nano-hydroxyapatite toothpaste and nano-hydroxyapatite plus 8% Arginine in dentine hypersensitivity intervention (Vano *et al*., 2018)(Anand *et al*., 2017). Table 3 represent clinical trials with polysaccharides based Nano-material.

**Table 3: Clinical trials with long chain polymeric carbohydratebased Nano-material**

|  |  |  |  |
| --- | --- | --- | --- |
| **Product** | **Clinical trial** | **Application** | **Reference** |
| Nano-Hydroxyapatite Toothpaste | Double Blind Randomized Clinical Trial | Dentine hypersensitivity | (Vano *et al*., 2018) |
| Nano-hydroxyapatite and 8% Arginine | Double Blind Randomized Clinical Trial. | Dentine hypersensitivity | (Anand *et al*., 2017) |
| Nanofibrillar cellulose wound dressing | Preliminary Clinical trial | Wound healing | (Hakkarainen *et al*., 2016) |
| Tinidazole functionalized homogeneous electrospun chitosan/poly (-caprolactone) hybrid nanofiber membrane | Preliminary Clinical trial | Chronic periodontitis | (Khan *et al*., 2017) |

**Conclusion**

Polymeric carbohydrate molecules consist of long chains of monosaccharide or disaccharide units, that are linked together covalently by glycosidic linkages.These are abundantly available and have potential to be used for synthesis, fabrication and structure. Their application ranges from biomaterials to electronics and other industrial uses. Polysaccharides also offer a “green” alternative to oil-based synthetic polymers.Formation ofnanoparticles from polysaccharides is achieved by ionic or covalent crosslinking, ion-complex andself-assembly after grafting of hydrophobic segments to the polymer backbone.In this regard, the choiceof the most suitable technique for nanoparticle production depends on the nature of the materials such ascharges and polymer chain lengths. In coming days these will become potential candidatesfor the precisely targeted delivery of drugs and genes in treatment of different diseases.

**List of abbreviations**

ECM= Extra cellular matrix

ESCs= Embryonic stem cells

HOB= Normal human osteoblasts

TiO2= Titanium dioxide

iPSCs= Induced pluripotent stem cells

FTIR= Fourier-transform infrared spectroscopy

XRD= X-ray crystallography

SEM= Scanning electron microscope

ESR= Electron Spin Resonance (ESR) Microscopy

FESEM= Field Emission Scanning Electron Microscope

PVA= Polyvinyl alcohol

TEM=Transmission electron microscopy

PCL-PEG-PCL/EA=poly(ɛ-caprolactone)-poly(ethylene glycol)-poly(ɛ-caprolactone)

nBGC= nano bioactive glass ceramic particles

HA= hyaluronicacid

PLGA= poly (d, l-lactide-co-glycolide acid)

AF= Annulus fibrosus

**Reference**

Aadil, K. R., Nathani, A., Sharma, C. S., Lenka, N., and Gupta, P. (2019). Investigation of poly(vinyl) alcohol-gellan gum based nanofiber as scaffolds for tissue engineering applications. Journal of Drug Delivery Science and Technology, *54*(June), 101276. https://doi.org/10.1016/j.jddst.2019.101276

Anand, S., Rejula, F., Sam, J. V. G., Christaline, R., Nair, M. G., and Dinakaran, S. (2017). Comparative Evaluation of Effect of Nano-hydroxyapatite and 8% Arginine Containing Toothpastes in Managing Dentin Hypersensitivity: Double Blind Randomized Clinical Trial. *Acta Medica (Hradec Kralove, Czech Republic)*, *60*(3), 114–119. https://doi.org/10.14712/18059694.2018.3

Anirudhan, T. S., and Rejeena, S. R. (2014). Aminated β -Cyclodextrin-Modified-Carboxylated Magnetic Cobalt/Nanocellulose Composite for Tumor-Targeted Gene Delivery. *Journal of Applied Chemistry*, *2014*, 1–10. https://doi.org/10.1155/2014/184153

Aslam, M. S., and Ahmad, M. S. (2016). Worldwide Importance of Medicinal Plants: Current and Historical Perspectives. *Recent Advances in Biology and Medicine*, *02*, 88. https://doi.org/10.18639/RABM.2016.02.338811

Awad, N. K., Edwards, S. L., and Morsi, Y. S. (2017). A review of TiO2 NTs on Ti metal: Electrochemical synthesis, functionalization and potential use as bone implants. *Materials Science and Engineering: C*, *76*, 1401–1412. https://doi.org/10.1016/j.msec.2017.02.150

Beg, S., Rahman, M., Jain, A., Saini, S., Midoux, P., Pichon, C., … Akhter, S. (2016). Nanoporous metal organic frameworks as hybrid polymer-metal composites for drug delivery and biomedical applications. *Drug Discovery Today*. https://doi.org/10.1016/j.drudis.2016.10.001

Cimpean, A., Neacsu, P., Mazare, A., and Schmuki, P. (2015). Attenuation of the macrophage inflammatory activity by TiO2 nanotubes via inhibition of MAPK and NF-andamp;kappa;B pathways. *International Journal of Nanomedicine*, 6455. https://doi.org/10.2147/IJN.S92019

Costa, L. M. M., de Olyveira, G. M., Cherian, B. M., Leão, A. L., de Souza, S. F., and Ferreira, M. (2013). Bionanocomposites from electrospun PVA/pineapple nanofibers/Stryphnodendron adstringens bark extract for medical applications. *Industrial Crops and Products*, *41*(1), 198–202. https://doi.org/10.1016/j.indcrop.2012.04.025

Ding, X., Li, X., Li, C., Qi, M., Zhang, Z., Sun, X., … Zhou, Y. (2019). Chitosan/Dextran Hydrogel Constructs Containing Strontium-Doped Hydroxyapatite with Enhanced Osteogenic Potential in Rat Cranium. *ACS Biomaterials Science* and *Engineering*, *5*(9), 4574–4586. https://doi.org/10.1021/acsbiomaterials.9b00584

Freier, T., Montenegro, R., Shan Koh, H., and Shoichet, M. S. (2005). Chitin-based tubes for tissue engineering in the nervous system. *Biomaterials*, *26*(22), 4624–4632. https://doi.org/10.1016/j.biomaterials.2004.11.040

Fricain, J. C., Schlaubitz, S., Le Visage, C., Arnault, I., Derkaoui, S. M., Siadous, R., … Amédée, J. (2013). A nano-hydroxyapatite – Pullulan/dextran polysaccharide composite macroporous material for bone tissue engineering. *Biomaterials*, *34*(12), 2947–2959. https://doi.org/10.1016/j.biomaterials.2013.01.049

Guo, T., Yang, X., Deng, J., Zhu, L., Wang, B., and Hao, S. (2019). Keratin nanoparticles-coating electrospun PVA nanofibers for potential neural tissue applications. *Journal of Materials Science: Materials in Medicine*, *30*(1), 9. https://doi.org/10.1007/s10856-018-6207-5

Habibi, Y., Lucia, L. A., and Rojas, O. J. (2010). Cellulose Nanocrystals: Chemistry, Self-Assembly, and Applications. *Chemical Reviews*, *110*(6), 3479–3500. https://doi.org/10.1021/cr900339w

Hakkarainen, T., Koivuniemi, R., Kosonen, M., Escobedo-Lucea, C., Sanz-Garcia, A., Vuola, J., … Kavola, H. (2016). Nanofibrillar cellulose wound dressing in skin graft donor site treatment. *Journal of Controlled Release*, *244*, 292–301. https://doi.org/10.1016/j.jconrel.2016.07.053

He, H., Koh, M. J., Lee, H. Y., and Ang, S. Bin. (2020). Pilot study of a customized nanotextile wet garment treatment on moderate and severe atopic dermatitis: A randomized clinical trial. *Pediatric Dermatology*, *37*(1), 52–57. https://doi.org/10.1111/pde.13981

Hernandes, L., Pereira, L. M. da S., Palazzo, F., and Mello, J. C. P. de. (2010). Wound-healing evaluation of ointment from Stryphnodendron adstringens (barbatimão) in rat skin. *Brazilian Journal of Pharmaceutical Sciences*, *46*(3), 431–436. https://doi.org/10.1590/S1984-82502010000300005

Hokmabad, V. R., Davaran, S., Aghazadeh, M., Alizadeh, E., Salehi, R., and Ramazani, A. (2019). Effect of incorporating Elaeagnus angustifolia extract in PCL-PEG-PCL nanofibers for bone tissue engineering. *Frontiers of Chemical Science and Engineering*, *13*(1), 108–119. https://doi.org/10.1007/s11705-018-1742-7

Hu, Y., Chen, J., Fan, T., Zhang, Y., Zhao, Y., Shi, X., and Zhang, Q. (2017). Biomimetic mineralized hierarchical hybrid scaffolds based on in situ synthesis of nano-hydroxyapatite/chitosan/chondroitin sulfate/hyaluronic acid for bone tissue engineering. *Colloids and Surfaces B: Biointerfaces*, *157*, 93–100. https://doi.org/10.1016/j.colsurfb.2017.05.059

Ismail, N. A., Mat Amin, K. A., and Razali, M. H. (2018). Novel gellan gum incorporated TiO2 nanotubes film for skin tissue engineering. *Materials Letters*, *228*, 116–120. https://doi.org/10.1016/j.matlet.2018.05.140

Jin, G., Prabhakaran, M. P., Kai, D., Annamalai, S. K., Arunachalam, K. D., and Ramakrishna, S. (2013). Tissue engineered plant extracts as nanofibrous wound dressing. *Biomaterials*, *34*(3), 724–734. https://doi.org/10.1016/j.biomaterials.2012.10.026

Jin, R., Moreira Teixeira, L. S., Dijkstra, P. J., Karperien, M., van Blitterswijk, C. A., Zhong, Z. Y., and Feijen, J. (2009). Injectable chitosan-based hydrogels for cartilage tissue engineering. *Biomaterials*, *30*(13), 2544–2551. https://doi.org/10.1016/j.biomaterials.2009.01.020

Keskin, S., and Kızılel, S. (2011). Biomedical Applications of Metal Organic Frameworks. *Industrial* and *Engineering Chemistry Research*, *50*(4), 1799–1812. https://doi.org/10.1021/ie101312k

Khan, G., Yadav, S. K., Patel, R. R., Kumar, N., Bansal, M., and Mishra, B. (2017). Tinidazole functionalized homogeneous electrospun chitosan/poly (ε-caprolactone) hybrid nanofiber membrane: Development, optimization and its clinical implications. *International Journal of Biological Macromolecules*, *103*, 1311–1326. https://doi.org/10.1016/j.ijbiomac.2017.05.161

Kumar, A., Rao, K. M., and Han, S. S. (2017). Development of sodium alginate-xanthan gum based nanocomposite scaffolds reinforced with cellulose nanocrystals and halloysite nanotubes. *Polymer Testing*, *63*, 214–225. https://doi.org/10.1016/j.polymertesting.2017.08.030

Kusindarta, D. L., and Wihadmadyatami, H. (2018). The Role of Extracellular Matrix in Tissue Regeneration. In *Tissue Regeneration*. InTech. https://doi.org/10.5772/intechopen.75728

Li, Q., Niu, Y., Xing, P., and Wang, C. (2018). Bioactive polysaccharides from natural resources including Chinese medicinal herbs on tissue repair. *Chinese Medicine*, *13*(1), 7. https://doi.org/10.1186/s13020-018-0166-0

Li, Y., Wang, Y., Ye, J., Yuan, J., and Xiao, Y. (2016). Fabrication of poly(ε-caprolactone)/keratin nanofibrous mats as a potential scaffold for vascular tissue engineering. *Materials Science and Engineering: C*, *68*, 177–183. https://doi.org/10.1016/j.msec.2016.05.117

Li, Z., Ramay, H. R., Hauch, K. D., Xiao, D., and Zhang, M. (2005). Chitosan–alginate hybrid scaffolds for bone tissue engineering. *Biomaterials*, *26*(18), 3919–3928. https://doi.org/10.1016/j.biomaterials.2004.09.062

Liang, R., Wei, M., Evans, D. G., and Duan, X. (2014). Inorganic nanomaterials for bioimaging, targeted drug delivery and therapeutics. *Chem. Commun.*, *50*(91), 14071–14081. https://doi.org/10.1039/C4CC03118K

Liu, M., Zheng, H., Chen, J., Li, S., Huang, J., and Zhou, C. (2016). Chitosan-chitin nanocrystal composite scaffolds for tissue engineering. *Carbohydrate Polymers*, *152*, 832–840. https://doi.org/10.1016/j.carbpol.2016.07.042

Liu, Y., and Chan-Park, M. B. (2009). Hydrogel based on interpenetrating polymer networks of dextran and gelatin for vascular tissue engineering. *Biomaterials*, *30*(2), 196–207. https://doi.org/10.1016/j.biomaterials.2008.09.041

Luo, Y., Li, Y., Qin, X., and Wa, Q. (2018). 3D printing of concentrated alginate/gelatin scaffolds with homogeneous nano apatite coating for bone tissue engineering. *Materials* and *Design*, *146*, 12–19. https://doi.org/10.1016/j.matdes.2018.03.002

Ma, L. (2003). Collagen/chitosan porous scaffolds with improved biostability for skin tissue engineering. *Biomaterials*, *24*(26), 4833–4841. https://doi.org/10.1016/S0142-9612(03)00374-0

Mahboubi, M. (2018). Elaeagnus angustifolia and its therapeutic applications in osteoarthritis. *Industrial Crops and Products*, *121*, 36–45. https://doi.org/10.1016/j.indcrop.2018.04.051

Martínez Ávila, H., Schwarz, S., Rotter, N., and Gatenholm, P. (2016). 3D bioprinting of human chondrocyte-laden nanocellulose hydrogels for patient-specific auricular cartilage regeneration. *Bioprinting*, *1*–*2*, 22–35. https://doi.org/10.1016/j.bprint.2016.08.003

Martins, A. M., Eng, G., Caridade, S. G., Mano, J. F., Reis, R. L., and Vunjak-Novakovic, G. (2014). Electrically Conductive Chitosan/Carbon Scaffolds for Cardiac Tissue Engineering. *Biomacromolecules*, *15*(2), 635–643. https://doi.org/10.1021/bm401679q

Mokhtarzadeh, A., Alibakhshi, A., Hejazi, M., Omidi, Y., and Ezzati Nazhad Dolatabadi, J. (2016). Bacterial-derived biopolymers: Advanced natural nanomaterials for drug delivery and tissue engineering. *TrAC - Trends in Analytical Chemistry*, *82*(June), 367–384. https://doi.org/10.1016/j.trac.2016.06.013

Mokhtarzadeh, A., Alibakhshi, A., Yaghoobi, H., Hashemi, M., Hejazi, M., and Ramezani, M. (2016). Recent advances on biocompatible and biodegradable nanoparticles as gene carriers. *Expert Opinion on Biological Therapy*, *16*(6), 771–785. https://doi.org/10.1517/14712598.2016.1169269

Nabavinia, M., Khoshfetrat, A. B., and Naderi-Meshkin, H. (2019). Nano-hydroxyapatite-alginate-gelatin microcapsule as a potential osteogenic building block for modular bone tissue engineering. *Materials Science and Engineering C*, *97*(November 2018), 67–77. https://doi.org/10.1016/j.msec.2018.12.033

Nguyen, D., Hgg, D. A., Forsman, A., Ekholm, J., Nimkingratana, P., Brantsing, C., … Simonsson, S. (2017). Cartilage Tissue Engineering by the 3D Bioprinting of iPS Cells in a Nanocellulose/Alginate Bioink. *Scientific Reports*, *7*(1), 1–10. https://doi.org/10.1038/s41598-017-00690-y

Nikpour, P., Salimi-Kenari, H., Fahimipour, F., Rabiee, S. M., Imani, M., Dashtimoghadam, E., and Tayebi, L. (2018). Dextran hydrogels incorporated with bioactive glass-ceramic: Nanocomposite scaffolds for bone tissue engineering. *Carbohydrate Polymers*, *190*(March), 281–294. https://doi.org/10.1016/j.carbpol.2018.02.083

Ojansivu, M., Rashad, A., Ahlinder, A., Massera, J., Mishra, A., Syverud, K., … Mustafa, K. (2019). Wood-based nanocellulose and bioactive glass modified gelatin–alginate bioinks for 3D bioprinting of bone cells. *Biofabrication*, *11*(3), 035010. https://doi.org/10.1088/1758-5090/ab0692

Pagis, C., Ferbinteanu, M., Rothenberg, G., and Tanase, S. (2016). Lanthanide-Based Metal Organic Frameworks: Synthetic Strategies and Catalytic Applications. *ACS Catalysis*. https://doi.org/10.1021/acscatal.6b01935

Pan, J., Liu, N., Sun, H., and Xu, F. (2014). Preparation and Characterization of Electrospun PLCL/Poloxamer Nanofibers and Dextran/Gelatin Hydrogels for Skin Tissue Engineering. *PLoS ONE*, *9*(11), e112885. https://doi.org/10.1371/journal.pone.0112885

Pereira, D. R., Silva-Correia, J., Oliveira, J. M., Reis, R. L., Pandit, A., and Biggs, M. J. (2018). Nanocellulose reinforced gellan-gum hydrogels as potential biological substitutes for annulus fibrosus tissue regeneration. *Nanomedicine: Nanotechnology, Biology and Medicine*, *14*(3), 897–908. https://doi.org/10.1016/j.nano.2017.11.011

Pötzinger, Y., Rabel, M., Ahrem, H., Thamm, J., Klemm, D., and Fischer, D. (2018). Polyelectrolyte layer assembly of bacterial nanocellulose whiskers with plasmid DNA as biocompatible non-viral gene delivery system. *Cellulose*, *25*(3), 1939–1960. https://doi.org/10.1007/s10570-018-1664-z

Ranjbar-Mohammadi, M. (2018). Characteristics of aloe vera incorporated poly(ε-caprolactone)/gum tragacanth nanofibers as dressings for wound care. *Journal of Industrial Textiles*, *47*(7), 1464–1477. https://doi.org/10.1177/1528083717692595

Rehm, B. H. A. (2010). Bacterial polymers: biosynthesis, modifications and applications. *Nature Reviews Microbiology*, *8*(8), 578–592. https://doi.org/10.1038/nrmicro2354

Ribeiro, M. P., Morgado, P. I., Miguel, S. P., Coutinho, P., and Correia, I. J. (2013). Dextran-based hydrogel containing chitosan microparticles loaded with growth factors to be used in wound healing. *Materials Science and Engineering: C*, *33*(5), 2958–2966. https://doi.org/10.1016/j.msec.2013.03.025

Riva, R., Ragelle, H., des Rieux, A., Duhem, N., Jérôme, C., and Préat, V. (2011). Chitosan and Chitosan Derivatives in Drug Delivery and Tissue Engineering. In *Advances in Polymer Science* (pp. 19–44). https://doi.org/10.1007/12\_2011\_137

Schaate, A., Roy, P., Godt, A., Lippke, J., Waltz, F., Wiebcke, M., and Behrens, P. (2011). Modulated synthesis of Zr-based metal-organic frameworks: From nano to single crystals. *Chemistry - A European Journal*, *17*(24), 6643–6651. https://doi.org/10.1002/chem.201003211

Sharma, C., Dinda, A. K., Potdar, P. D., Chou, C. F., and Mishra, N. C. (2016). Fabrication and characterization of novel nano-biocomposite scaffold of chitosan-gelatin-alginate-hydroxyapatite for bone tissue engineering. *Materials Science and Engineering C*, *64*, 416–427. https://doi.org/10.1016/j.msec.2016.03.060

Singh, B. N., Veeresh, V., Mallick, S. P., Jain, Y., Sinha, S., Rastogi, A., and Srivastava, P. (2019). Design and evaluation of chitosan/chondroitin sulfate/nano-bioglass based composite scaffold for bone tissue engineering. *International Journal of Biological Macromolecules*, *133*, 817–830. https://doi.org/10.1016/j.ijbiomac.2019.04.107

Stachewicz, U., Qiao, T., Rawlinson, S. C. F., Almeida, F. V., Li, W.-Q., Cattell, M., and Barber, A. H. (2015). 3D imaging of cell interactions with electrospun PLGA nanofiber membranes for bone regeneration. *Acta Biomaterialia*, *27*, 88–100. https://doi.org/10.1016/j.actbio.2015.09.003

Thein-Han, W. W., and Misra, R. D. K. (2009). Biomimetic chitosan–nanohydroxyapatite composite scaffolds for bone tissue engineering. *Acta Biomaterialia*, *5*(4), 1182–1197. https://doi.org/10.1016/j.actbio.2008.11.025

Vano, M., Derchi, G., Barone, A., Pinna, R., Usai, P., and Covani, U. (2018). Reducing dentine hypersensitivity with nano-hydroxyapatite toothpaste: a double-blind randomized controlled trial. *Clinical Oral Investigations*, *22*(1), 313–320. https://doi.org/10.1007/s00784-017-2113-3

Vashisth, P., and Pruthi, V. (2016). Synthesis and characterization of crosslinked gellan/PVA nanofibers for tissue engineering application. *Materials Science and Engineering: C*, *67*, 304–312. https://doi.org/10.1016/j.msec.2016.05.049

Wang, J., Tian, L., He, L., Chen, N., Ramakrishna, S., So, K.-F., and Mo, X. (2018). Lycium barbarum polysaccharide encapsulated Poly lactic-co-glycolic acid Nanofibers: cost effective herbal medicine for potential application in peripheral nerve tissue engineering. *Scientific Reports*, *8*(1), 8669. https://doi.org/10.1038/s41598-018-26837-z

Wang, S., McGuirk, C. M., Ross, M. B., Wang, S., Chen, P., Xing, H., … Mirkin, C. A. (2017). General and Direct Method for Preparing Oligonucleotide-Functionalized Metal–Organic Framework Nanoparticles. *Journal of the American Chemical Society*, *139*(29), 9827–9830. https://doi.org/10.1021/jacs.7b05633

Wang, X., Liu, L.-H., Ramstrom, O., and Yan, M. (2009). Engineering Nanomaterial Surfaces for Biomedical Applications. *Experimental Biology and Medicine*, *234*(10), 1128–1139. https://doi.org/10.3181/0904-MR-134

Wang, Xiaoyu, Li, Z., Shi, T., Zhao, P., An, K., Lin, C., and Liu, H. (2017). Injectable dextran hydrogels fabricated by metal-free click chemistry for cartilage tissue engineering. *Materials Science and Engineering: C*, *73*, 21–30. https://doi.org/10.1016/j.msec.2016.12.053

Zheng, Y., Monty, J., and Linhardt, R. J. (2015). Polysaccharide-based nanocomposites and their applications. *Carbohydrate Research*, *405*, 23–32. https://doi.org/10.1016/j.carres.2014.07.016