
**Reviewer’s Comments**

****

**THE USE OF COMBINATION OF LUTEIN-ZEAXANTHIN FROM EGG YOLK AS A PREVENTIVE MEASURE AGAINST *COMPUTER VISION SYNDROME* (CVS) BERBASIS *HYDROGEL EYE MASK***

**ABSTRACT**

*Computer Vision Syndrome* (CVS) is a collection of symptoms related to eye disorders due to the use of computer-based digital devices. So substantial protection is needed against damage caused by exposure to blue light by digital devices. Lutein and zeaxanthin are carotenoids that contain antioxidants so that they can overcome inflammation, have a calming effect and can maintain eye health. The purpose of this research is to produce a topical preparation in the form of a *hydrogel eye mask* from egg yolk which is useful for overcoming *Computer Vision Syndrome* (CVS). This study formulated three formulas with the active ingredients of egg yolk extract 400µg, 600µg and 800µg using 8.75 g of Na-alginate base and 3.75 g of xanthan gum.Evaluation of the preparations included organoleptic tests, weight and size, pH, swellability, shrinkage, homogeneity, viscosity, spreadability, adhesion and stability tests. The results of the evaluation of thepreparations *hydrogel eye mask* in the three formulas showed good physical characteristics and stability. The results of the evaluation that have been carried out show that the organoleptic test has no changes in color, odor and shape. Test the appropriate weight and size under the eye area. The pH test of the three formulas before storage was 7.3±0.15, 7.1±0.05, 7.1±0.17 and after storage 7.5±0.1, 7.4±0.1, 7.2±0.2. The expansion and shrinkage test showed an increase in weight every hour and a decrease in weight every 10 minutes. The homogeneity test showed the three formulas were homogeneous. The viscosity test is in a good range. The dispersion test of the three formulas before storage was 5.13±0.2, 5.07±0.15 and 5.18±0.28 cm and after storage 5.05±0.13, 5.20±0.32, 5.11±0.22 cm. The adhesion of each formula before storage was 4.23±0.51, 3.27±0.84, 3.28±0.62 seconds and after storage was 3.24±0.38, 3.26±0.15, 2.96±0.77 seconds. The three formulas produced have good pharmaceutical characteristics and stability so that they can be used to treat *Computer Vision Syndrome* (CVS).

**Keywords**: *Computer Vision Syndrome* (CVS), lutein-zeaxanthin, egg yolk, *hydrogeleye mask*

**INTRODUCTION**

Since COVID-19 pandemic has had a considerable impact on society. One of the major impacts that affect the community is the large-scale social restrictions that cause all community activities to be restricted. During the COVID-19 pandemic, the government imposed *Work From Home*

(WFH) for workers and distancelearning for students (Rizqullah, 2020).

So that children, teenagers and adults can spend most of their time in front of a computer or cell phone screen. According to Bhattacharya (2020) these devices can cause damage by emitting high energy waves that can penetrate the eye and can eventually contribute to photochemical damage to retinal cells, which can make a person susceptible to various eye problems ranging from dry eyes to age-related macular degeneration.

Eye strain caused by digital devices or also known as *Computer Vision Syndrome* (CVS) is the most common problem related to prolonged use of digital devices that can cause complaints such as dry eyes, itching, foreign body sensation, watering, blurred vision, and pain. Symptoms can be caused by poor lighting, glare and reflections on the screen, improper viewing distance, poor posture, uncorrected vision problems, or a combination of these factors head (Mohan et al., 2020).

The main cause of CVS is exposure to blue light sourced from LED lighting from digital devices so that exposure to blue light can have a negative effect on eye strain, psychological stress and overall health and sleep quality (Akinbinu and Mashalla, 2014). So substantial protection is needed against damage caused by exposure to blue light by digital devices. Lutein and Zeaxanthin are known as carotenoids which contain strong antioxidants so that they can overcome inflammation, have a calming effect and can maintain eye health (Bruno and Ahg, 2017).

Lutein and zeaxanthin are carotenoids with antioxidant properties found in egg yolks (Handelman et al., 2018). Some researchers say that these carotenoids can not be synthesized directly by humans. Therefore, it depends on the consumption of certain fruits, vegetables or animal products such as eggs (Calvo, 2014). other food sources (Kelly et al., 2014).

The use of carotenoids lutein and zeaxanthin which contain antioxidants in overcoming *Computer Vision Syndrome* (CVS) is formulated into apreparation*hydrogel eye mask*. Hydrogel masks are one of the most commonly used mask ingredients because of their high water content. The hydrophilic base will form a strong matrix so that the active substance is easily delivered to the eye bags. Thus it can provide high effectiveness (Lim et al., 2010). So in this study, aformulation was made *hydrogel eye mask* from egg yolk extract containing the carotenoids lutein and zeaxanthin. The focus of this research is to obtain apreparation*hydrogel eye mask* that can overcome *Computer Vision Syndrome* (CVS) with good pharmaceutical stability.

**MATERIALS AND METHODS**

**MATERIALS**

Extract carotenoid compounds lutein-zeaxanthin chicken egg yolk, n-hexane, acetone, toluene, ethanol, Na2SO4 10%, distilled water, Na-Alginate, Xanthan-gum, glycerin, propyl paraben, methyl paraben, propylene glycol, calcium chloride, essence .

**Preparation of Tools and Materials**

Tools and materials of this research are prepared in accordance with the needs of the research to be carried out.

**Preparation of Lutein-Zeaxanthin Extract**

Eggs were stored overnight for 7 days at 18o C. The yolks were separated from the egg whites manually and rolled on moistened filter paper to remove any remaining albumin and chalaza adherents. The egg yolks were then combined and homogenized in a blender at a speed of level 1 for 60 seconds (Wenzel et al., 2010).

**Carotenoid-Lutein ZeaxanthinExtraction**

Carotenoids were extracted from the prepared samples (1 g egg yolk homogenate or 2 mL serum) by adding 30 mL of hexane:acetone:toluene:ethanol (10:7:7:6) and incubating overnight at room temperature. Then add hexane (30 `mL) and 10% Na2S04 to increase the total volume in a 100 mL volumetric flask. This mixture was mixed and allowed to stand for 1 hour

before the 10 mL aliquot of the hexane layer evaporated. The extracted carotenoids were then stored overnight in a dark room at 20⸰C (Scaeffer et al., 1987).

**Preparation of The Hydrogel Eye Mask**

Mask by preparing distilled water in a 1 liter beaker then adding Na-Alginate which has been weighed while stirring at medium speed until a gel base is formed. Xanthan gum is mixed with glycerin, then put into a gel base. Stirring is continued at a constant speed. Then added lutein-zeaxanthin compound extract. The solution was stirred until dissolved and homogeneous. Put into a gel base, stirred at a constant speed. Then Propyl paraben and methyl paraben were dissolved in propylene glycol, put into a beaker containing a gel base little by little. Then the gel is poured into a mold with a diameter of 10 cm. The weight of the gel that is poured must have the same weight as each other, which is 50 g. The mold is then immersed in a solution of distilled water containing calcium chloride with a concentration of 0.5g/100mL (w/v). Immersion was carried out for 60 minutes. After 60 minutes, a hydrogel with a solid mass is formed, the formed mass is washed with distilled water. Then dried at room temperature. Then the hydrogel is molded according to the shape that is adapted to the under-eye area. The hydrogel mask is stored in a closed package containing a small amount of propylene glycol solution (Okwani et al., 2020).

**Evaluation of hydrogel mask preparations**

**Organoleptic**

The preparations were observed for size, shape, color, and odor as well as changes in color and odor changes (Okwani et al., 2020).

|  |  |  |  |
| --- | --- | --- | --- |
| Compotition | F1 | F2 | F3 |
| Egg yolk caratenoid extract | 400 | 600 | 800 |
| Na-alginaet (grams) | 8,75 | 8,75 | 8,75 |
| Xanthan gum (grams) | 3,75 | 3,75 | 3,75 |
| Propylene glycol (grams) | 7,5 | 7,5 | 7,5 |
| Calcium chloride (grams) | 0,5 | 0,5 | 0,5 |
| Glycerin (grams) | 13,75 | 13,75 | 13,75 |
| Methyl paraben (grams) | 2,5 | 2,5 | 2,5 |
| Propyl paraben (grams) | 1,25 | 1,25 | 1,25 |
| Essence (drops) | 3 | 3 | 3 |
| Aquadest (mL) | ad 250 | ad 250 | ad 250 |

Table 1. Hydrogel mask formulation

**Hydrogel Eye Mask Weight and Size**

Evaluation of the weight and thickness of the mask, hydrogel masks were taken and weighed one by one. The weight of the hydrogel mask was measured using a digital scale, while the length, width, and thickness of the hydrogel mask were measured using a caliper (Okwani et al., 2020).

**Hydrogel Eye Mask Surface pH Test**

The surface pH of the hydrogel mask was measured using apH meter *portable*.

**Expandability Hydrogel Eye Mask**

The hydrogel mask was weighed and put into a beaker containing 30 ml of distilled water solution. Mask pieces were weighed at 3, 9, 12, 24, 48, 72, and 1 week. (Okwani et al., 2020): Swelling power = Wn-Wo × 100 % Wo. Note: Wn = weight of hydrated mask; Wo = weight of dry mask before hydration

**Shrinkage Hydrogel Mask**

The hydrogel mask that had solidified area and weight were measured every 10 minutes for 2 hours from the start of the experiment. The time the area shrinkage occurs is recorded.

**Homogeneity Test**

All hydrogel preparations developed were tested for their homogeneity visually. The homogeneity test was carried out by applying the hydrogel eye mask formula on the object glass. The hydrogel was placed on a slide and then covered with a deg glass to see the clarity and presence of aggregates in the hydrogel preparation.

**Viscosity Test**

The Brookfield Viscometer uses spindle number 6 to determine the viscosity of each formula. The speed was increased from 12 rpm (*revolutions per minute*), 30 rpm, to 60 rpm and the viscosity test results were recorded in mPa.s (*millipascal-seconds*), the viscosity test was replicated three times and the average was calculated (YennyHarliantika and Noval, 2021).

**Spreadability Test**

Spreadability was measured with two glass plates, one glass plate was givena millimeter block base for easy observation and measurement and the other plate was used as a cover. The measurement of the dispersion of the hydrogel was carried out by placing 1 g of the hydrogel in the middle of the glass. Cover the hydrogel with a cover slip and a ballast with a total weight of 125 g for 1 minute, the diameter of the distribution area is calculated. Measurements were made 3 times of replication (Edy et al., 2016).

**Adhesion Test**

The adhesion test was carried out by weighing 1 gram of hydrogel placed on one glass plate and then covered with another glass plate. The glass plate was placed under 200g for 5 minutes. Record the time when the adhesive was released by lowering the load to 200 grams, the measurement was carried out 3 times.

**Stability Test**

Evaluation of stability was carried out by the accelerated method, namely by placing the gel preparation at a freezing temperature of -10⸰C (14⸰F) for 24 hours, then transferred again at room temperature around 25-29⸰C (77⸰F) for 24 hours using adevice. *climaticchambers*. Parameter testing was carried out before and after the accelerated storage treatment. The gel is declared stable if there is no significant difference to the observed parameter results

**Data analysis**

This research is an experimental laboratory scale and uses statistical analysis annova method.

**RESULTS AND DISCUSSION**

This research was started by extracting lutein and zeaxanthin from egg yolk. The egg yolk used is organic chicken egg yolk. Incubated chicken eggs in an incubator for 7 days at a temperature of 18°C before Carotene is extracted. Extraction of carotenoids using n-hexane, acetone, toluene and ethanol in the ratio (10:7:7:6) and incubated overnight at room temperature. Extraction was continued by adding n-hexane and 10% Na2SO4. Carotene is extracted is stored in a dark room at a temperature of 20°C before use.

The carotenoid extracts lutein and zeaxanthin contain powerful antioxidants that can reduce oxidative damage indirectly by absorption of light contained in the pigment epithelium of the retina, lens, ciliary body, and iris. In addition, the presence of oxidized metabolites suggests that lutein and zeaxanthin may protect against oxidative stress (Mares, 2016).

The carotenoid extracts of lutein and zeaxanthin are formulated in the form of *hydrogel eye mask* as much as 50 grams. Based on the preformulation, a formula was obtained using Na-alginate and xanthan gum as a base, glycerin and propylene glycol as *plasticizers*, and calcium chloride as a crosslinking agent. Treatment with various concentrations of carotenoids with variations of 400 g, 600 g and 800 g in each preparation with three replications. This is done to determine the preparation with the best concentration.

All components of the formula based on the preformulation were mixed using a mixer at medium speed for 60 minutes. The homogenized hydrogel was immersed in a calcium chloride solution with a concentration of 0.5% for 60 minutes. After the immersion process, a solid structure was obtained from the hydrogel, the mask was then printed and stored in a container containing a propylene glycol solution as a humectant so that the water in the hydrogel did not evaporate quickly during the storage process. Evaluation of the preparation was carried out by means of organoleptic observation, weight and size, pH test, and swelling, shrinkage, homogeneity test, dispersion test and adhesion test which were formed on the three formulations.

In organoleptic testing, the dosage form, color and odor were observed. The results obtained for each of the three formulas with three replications before and after accelerated storage obtained the same results. The three formulas have a pink color because the base used is Naalginate. The resulting color is not too bright so it is still quite comfortable to use. Another physical appearance is the consistency of semi-solid and odorless so that this hydrogel is quite soft and gives a cooling effect when used.

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| **Condition** | **Formula** | **Observation** | | |
| **Color** | **Form** | **Odor** |
| Before | F1 | Pink | Semi solid | Odorless |
| F2 | Pink | Semi solid | Odorless |
| F3 | Pink | Semi solid | Odorless |
| After | F1 | Pink | Semi solid | Odorless |
| F2 | Pink | Semi solid | Odorless |
| F3 | Pink | Semi solid | Odorless |

Table 2. *Hydrogel eye mask* organoleptic test results

Evaluation of weight and size was carried out using three formulas before and after accelerated storage. The evaluation of the weight and size of the *hydrogel eye mask* from the three formulations has almost the same weight, length, width and thickness and is quite good. After accelerated storage, there was no significant change to the length, width, weight and thickness of the *hydrogel eye mask*. The weight and size are adjusted to the area under the eyes with a size of 6 x 2.5 cm (length and width) (Okwani et al., 2020).

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Condition** | **Formula** | **Observation** | | | |
| **Weight (g)** | **Width (cm)** | **Length (cm)** | **Thickness (cm)** |
| Before | F1 (right and left) | 2.29±0.46/2.44±0.39 | 2.23±0.40/2.30±0.36 | 6.26±0.45/6.23±0.05 | 0.23±0.03/0.23±0.03 |
| F2 (right and left) | 3.10±0.24/3.02±0.04 | 2.20±0.10/2.033±0.23 | 6.33±0.25/6.23±0.40 | 3.28±0.13/3.25±0.13 |
| F3 (right and left) | 2.30±0.12/2.52±0.32 | 2.03±0.15/2.20 ± 0.43 | 3.28±0.13/3.25±0.10 | 2.23/0.05/2.16±0.05 |
| After | F1 (right and left i) | 2.33±0.32/2.50±0.30 | 2.23±0.32/2.26±0.37 | 6.23±0.20/6.26±0.05 | 0.20±0.10/0.20±0.10 |
| F2 (right and left | 3.04±0.16/3.00±0.10 | 2.23±0.05/1.96±0.37 | 6.43±0.20/6.53±0.30 | 3.21±0.16/3.21±0.16 |
| F3 (right and left) | 2.23±0.11/2.53±0.23 | 2.03±0.15/ 2.13±0.35 | 6.03±0.15/5.93±0.11 | 2.23±0.05/ 2.16±0.05 |

Table 3. Test results of weight and size of *hydrogel eye mask*

pH testing was carried out on the three formulas before and after accelerated storage. Testing pH using apH meter *portable*. The results obtained in each preparation showed that the pH of the preparation was in the *range* (7.1-7.3) before storage. While the pH of the preparation after storage was in the range (7.2-7.4) and there was an increase in pH but the pH of the preparation was still in the neutral pH range so that thepreparation was *hydrogel eye mask* safe to use.

Fig.1 Test results of pH *hydrogel eye mask*

Thepower of the *swellinghydrogel eye mask* in the three formulas before and after storage was accelerated with three replications, respectively, at 3, 9, 12, 24, 48, 72, and 1 week. The test results obtained that the hydrogel mass tends to increase with increasing time both before and after accelerated storage. According to Okwani*et al.,(*2020) the increase in hydrogel mass describes the amount of water absorbed and indicates that the hydrogel can absorb water. The hydrogel was allowed to swell for one week to see the swellability profile of the hydrogel.

The results of the swelling power measurement showed that the measurements from the 3rd hour to the first 1 week had an increase of up to 26% before storage, while after storage there was an increase of up to 25%.

Fig.2 The results of the test of the swelling power of the formula 1

Fig.3 The results of the test of the swelling power of the formula 2

Fig.4 The results of the test of the swelling power of the formula 3

The shrinkage of the *hydrogel eye mask was* carried out on three formulas with each replication before and after accelerated storage and left in an open room for two hours. *The hydrogel eye mask* experienced shrinkage from the first ten minutes which was marked by a decrease in the weight of the *hydrogel eye mask ±* 0.5grams every ten minutes and undergoes continuous shrinkage for up to two hours. According to Surini and Annisa(2017) shrinkage of hydrogel masks is caused by evaporation of water which indicates that *hydrogel eye masks* should be stored in closed container

Fig.5 The results of the shrinkage test formula 1

Fig.6 The results of the shrinkage test formula 1

Fig.6 The results of the shrinkage test formula 2

Fig.7 The results of the shrinkage test formula 2

Fig.8 The results of the shrinkage test formula 3

Fig.9 The results of the shrinkage test formula 3

Based on the homogeneity test before and after accelerated storage which was carried out on thepreparations *hydrogel eye mask* on the three formulas with three replications each, the results of the three formulas were homogeneous. Homogeneity was observed by looking at the clarity and there was no aggregate in thepreparation *hydrogel eye mask* which was carried out with three tests on each formula.

|  |  |  |
| --- | --- | --- |
| **Formula** | **Homogeneity Test** | |
| **Before** | **After** |
| F1 | Homogeneous | Homogeneous |
| F2 | Homogeneous | Homogeneous |
| F3 | Homogeneous | Homogeneous |

Table 3. Test results of homogeneity of *hydrogel eye mask*

Viscosity test *hydrogel eye mask* before and after storage is accelerated obtained test results on all three formulas with each of the three replication using a *viscometer brookfield*at a speed of 12 rpm showed that the preparation *hydrogel eye mask* has a viscosity that is as good between the three formulas because they are within the range of viscosities good according to the literature. According to Edy*et al.,* (2016) the viscosity of a good hydrogel preparation is in the range of 50 dPa.S – 400 dPa.S. The viscosity value will produce a hydrogel that is not too liquid and not too thick which is in dPa.S units (1 Poise = 1 dPa.S).

Fig.10 *hydrogel eye mask* viscosity test results

Based on the results of the test results of thepreparations *hydrogel eye mask* before and after accelerated storage in the three formulas with three replications each, it was found that the three preparations had good dispersion power according to the standard range of a good hydrogel formula. According to Edy*et al.,* (2017) the standard dispersion range of a good hydrogel formulation is between 5-7 cm.

Fig.10 *hydrogel eye mask* dispersion test results

The adhesion test was carried out by placing a 200g load on the threepreparations *hydrogel eye mask* with three replications each. The results obtained from the adhesion test show that the formula has good adhesion and meets the standard of good adhesion range. According to Harliatika and Noval(2021) the range of good adhesion is in the range of 2.00-30.00 seconds.

Fig.11 *hydrogel eye mask* adhesion test results

**CONCLUSION**

The formulation *hydrogel eye mask* containing lutein-zeaxanthin from egg yolk extract produced a fairly good preparation. Based on the tests that have been carried out, the three formulas obtained are good preparations and meet the quality parameters that have been set. The appearance of the hydrogel is subjectively comfortable to see and use because it has a pink color and is not too bright and has good physical stability so that it can be used as a preparation to overcome *Computer Vision Syndrome* (CVS).

**CONFLICT OF INTEREST:**

No conflict of interest associated with this work

**ACKNOWLEDGMENTS:**

The author would like to thank the Ministry of Education and Culture of the Republic of Indonesia and the Indonesian Muslim University for providing space for us to participate in the Student Creativity Program (PKM) and conduct this research. Thanks are also conveyed to the Head of the Pharmacy Study Program and the Head of the Laboratory for the permission and facilities to use the laboratory during the research.

**Author’s Contribution**

**REFERENCES**

Akinbinu, T.R., Mashalla, Y.J., 2014. Impact of computer technology on health : Computer Vision Syndrome ( CVS ). *Med. Pract. Rev.* 5, 20–30.

Bruno, B.G., Ahg, R.H., 2017. Zeaxanthin : Huntingt. Coll. *Heal. Sci*. 32–35.

Bhattacharya, S., 2020. Sheikh Mohd Saleem, Amarjeet Singh, 2020. Symposium Recent advances and challenges in the management of retinoblastoma Globe ‑savingTreatments. *BMC Ophthalmol.* 68, 1709–1710.

Calvo, M.M., 2014. Lutein : A Valuable Ingredient of Fruit and Vegetables Lutein : A Valuable Ingredient of Fruit. Crit. *Rev. Food Sci.* Nutr. 45: 37–41.

Edy, H.J., Marchaban, Wahyuono, S., Nugroho, A.E., 2016. Formulasi dan Uji Sterilitas Hidrogel Herbal Ekstrak.*J. Ilm. Farm*. 5, 9–16.

Handelman, G.J., Nightingale, Z.D., Lichtenstein, A.H., Schaefer, E.J., Blumberg, J.B., 2018. Lutein and zeaxanthin concentrations in plasma after dietary supplementation with egg yolk 1 – 3. J. *Clin. Nutr*. 70:3–7.

Harlika Y dan Noval. 2021. Formulasi dan Evaluasi Hidrogel Ekstrak Etanol Daun Gaharu (*Aquilaria malacensis* Lamk.) dengan Kombinasi Basis Karbopol 940 dan HPMC K4M. *Journal of Pharmacy and Science*. 6(1):37-46

Kelly, E.R., Plat, J., Haenen, G.R.M.M., Kijlstra, A., Berendschot, T.T.J.M., 2014. The Effect of Modified Eggs and an Egg-Yolk Based Beverage on Serum Lutein and Zeaxanthin Concentrations and Macular Pigment Optical Density : Results from a Randomized Trial. *PLoS One* 9:1–9.

Lim KB, Hur W, Kim JY, Lee DH, 2010. US 2010/0112058 A1. United States

Mares, J., 2016. Lutein and Zeaxanthin Isomers in Eye Health and Disease. Annu. *Rev.Nutr.* 36:571–602

Mohan, A., Sen, P., Shah, C., Jain, E., Jain, S., 2020. Prevalence and risk factor assessment of digital eye strain among children using online e ‑ learning during the COVID ‑ 19 pandemic : Digital eye strain among kids (DESK study ‑ 1 ). *Indian J. Ophthalmol.* 69, 140–144.

Okwani, Y., Halid, N.A., Hasanuddin, S., Djunaidin, D., Hikmat, D.J., 2020. Formulasi Hydrogel Eye Mask Berbasis Ekstrak Limbah Kepala Udang Putih (Litopenaeus vannamei) Sebagai Suplemen dan Relaksasi Mata Lelah. *J. Mandala Pharmacon Indones*. 6: 111–117.

Rizqullah, R. 2020. Artikel Riview Tentang E-Larning dan Pembelajaran Jarak Jauh (PPJ) Saat Masa Pandemi. *Journal Education*

Scaeffer, J.L., Juliusz K, Tyczkowski, Carmen R. Parkhurst, Pat B. Hamilton, 1987. Carotenoid Composition of Serum and Egg Yolks of Hens Fed Diets Varying in Carotenoid Composition. *Poult. Sci*. 67: 608–614.

Wenzel, M., Seuss-Baum, I., Schlich, E., 2010. Influence of pasteurization, spray- And freeze-drying and storage on the carotenoid content in egg yolk. *J. Agric. Food Chem*. 58:1726–1731.

Yenny Harliantika, Noval, 2021. Formulasi dan Evaluasi Hidrogel Ekstrak Etanol Daun Gaharu (*Aquilaria malacensis* Lamk.) dengan Kombinasi Basis Karbopol 940 dan HPMC K4M. *J. Pharm. Sci*. 6, 37–46.